ISO‑Style Process Sheet

LEA‑Hyper‑Alloy – Manufacturing Process Specification

1 Scope

This process sheet specifies the manufacturing steps, temperature and time windows, and quality requirements for the production of a conductive aluminum‑copper‑magnesium alloy (LEA alloy).

The process applies to continuously cast, direct‑chill cast, extruded, and rolled semi‑finished products.

2 Normative References

The following referenced documents are indispensable for the application of this process sheet:

• 	EN 573 – Aluminium and aluminium alloys – Chemical composition

• 	EN 485 – Aluminium and aluminium alloy sheet, strip and plate – Mechanical properties

• 	ISO 6892‑1 – Metallic materials – Tensile testing

• 	ISO 6506‑1 – Metallic materials – Brinell hardness test

• 	ISO 1463 – Metallic coatings – Micrographic determination of thickness

3 Terms and Definitions

LEA alloy:

An aluminum‑based alloy containing 1.5–3.5 wt% Cu and 1.0–2.0 wt% Mg, designed for enhanced electrical conductivity combined with moderate to high mechanical strength.

4 Chemical Composition

The alloy shall comply with the following mass fraction limits:

5 Process Flow

5.1 Overview (formal arrow diagram)

Raw Material Preparation

↓

Melting (650–700 °C, 30–120 min)

↓

Casting (680–700 °C)

↓

Homogenization (optional: 480–520 °C, 4–12 h)

↓

Hot Forming (400–450 °C)

↓

Solution Heat Treatment (500–520 °C, 30–90 min)

↓

Quenching (water or air)

↓

Artificial Aging / Overaging (150–200 °C, 4–12 h)

↓

Final Machining

↓

Quality Inspection

5.2 Detailed Process Requirements

5.2.1 Melting

• 	Temperature: 650–700 °C

• 	Holding time: 30–120 min

• 	Atmosphere: air or optional inert gas (argon)

• 	Objective: complete dissolution of alloying elements

5.2.2 Casting

• 	Casting temperature: 680–700 °C

• 	Methods: continuous casting or direct‑chill casting

• 	Cooling: controlled, air‑ or mold‑cooled

5.2.3 Homogenization (optional but recommended)

• 	Temperature: 480–520 °C

• 	Duration: 4–12 h

• 	Purpose: reduction of segregation and microstructural homogenization

5.2.4 Hot Forming

• 	Entry temperature: 380–450 °C

• 	Process temperature: 400–450 °C

• 	Methods: extrusion or hot rolling

5.2.5 Solution Heat Treatment

• 	Temperature: 500–520 °C

• 	Duration: 30–90 min

• 	Purpose: formation of a supersaturated solid solution

5.2.6 Quenching

• 	Medium: water (10–40 °C) or air

• 	Purpose: retention of supersaturation

5.2.7 Artificial Aging / Overaging

• 	Temperature: 150–200 °C

• 	Duration: 4–12 h

• 	Purpose: adjustment of conductivity/strength balance

• 	Recommended settings:

• 	LEA‑90: higher T, longer t → maximum conductivity

• 	LEA‑100: intermediate T/t → balanced properties

• 	LEA‑120: lower T, shorter t → higher strength

6 Quality Requirements

6.1 Mechanical Properties

• 	Tensile strength (Rm): 180–320 MPa (depending on grade)

• 	Elongation (A): ≥ 8 %

• 	Hardness: 60–90 HB

6.2 Electrical Properties

• 	Electrical conductivity: 45–55 % IACS (depending on grade)

6.3 Microstructural Requirements

• 	Uniform grain structure

• 	Low porosity

• 	No coarse intermetallic precipitates

• 	Controlled precipitation morphology

7 Inspection and Testing

• 	Tensile test: ISO 6892‑1

• 	Hardness test: ISO 6506‑1

• 	Electrical conductivity: eddy‑current method

• 	Metallography: optical or SEM examination

• 	Dimensional inspection: per product specification

8 Marking and Traceability

Each batch shall be marked with:

• 	Alloy grade (LEA‑90 / LEA‑100 / LEA‑120)

• 	Melt number

• 	Production date

• 	Heat treatment condition

• 	Verified test results (Rm, A, HB, IACS)